Vital Pulp Therapy: “What’s New When Meeting An Old Friend?”

By

John F. Wisniewski, DMD, MS1, MS2

1MS in Dental Materials (Emphasis on Clinical Research), 2MS in Endodontics

Associate Professor – Specialist in Endodontist

Roseman College of Dental Medicine, South Jordan, UT

Vital Pulp Therapy Clinical Protocol

Clinical Magnification

- Required for inspection of pulp tissue at various stages.

Clinical Procedure

*Complete initial cavity preparation removing all peripheral decay.”

Upon deep decay removal:

- If pinpoint pulpal exposure, regardless of whether bleeding stops or not, place new #4 round surgical bur/diamond, extend 2 mm deeper and 2 mm wider.

- If larger pulp exposure, after decay removal, bleeding should stop on its own.

If not, conservative clinical adjuncts in attaining stoppage of pulpal bleeding may include:

(1)  gentle rinse with 3% sodium hypochlorite solution, or

(2) placement of a cotton pellet moistened with 3% sodium hypochlorite on the pulp exposure with light pressure.

If bleeding does not stop, place new #4 round surgical bur/diamond, and continue to remove pulp at 2 mm depths incrementally until bleeding stops.

- Once bleeding stops, place bioceramic material (Brassler’s RRM) directly on exposed pulp tissue. The bioceramic material should have a minimum thickness of 2 mm over the exposed pulpal tissue and should cover at least 2 mm of solid dentin surrounding the exposed pulp.

Utah Dental Association Annual Meeting

January 24, 2025               2:00pm-4:00pm